Optimization of Six-Membered Ring Aluminum Complexes in -Caprolactone Polymerization

Wei-Yi Lu,a‡ Yi-Chen Lin,b‡ Cheng-Jie Lian,be Kuo-Hui Wu,c Michael Y. Chiang,be Hsuan-Ying Chen,bde* Chu-Chieh Lin,a* and Bao-Tsan Koa*

a Department of Chemistry, National Chung Hsing University, Taichung 402, Taiwan, R.O.C.

b Department of Medicinal and Applied Chemistry, Kaohsiung Medical University, Kaohsiung 80708, Taiwan, R.O.C.

c Department of Chemistry, Graduate School of Science, The University of Tokyo, Tokyo 113-0033, Japan.

d Department of Medical Research, Kaohsiung Medical University Hospital, Kaohsiung 80708, Taiwan, R.O.C.

e Department of Chemistry, National Sun Yat-Sen University, Kaohsiung, Taiwan, 80424, R.O.C.

Electronic supplementary information available: Polymer characterization data, and details of the kinetic study.

Table of Contents

Table S1.	The kinetic study of polymerizations of -caprolactone using various Al complexes as catalysts……………………………………………………………………………...….. 2-6

Tables S2.	The kinetic study of polymerizations of -caprolactone using various concentration of LBu-morph-AlMe2 (5) as a catalyst……………….………………….…………………….…………………...….... 7-8

Figure S1. 	First-order kinetic plots of CL polymerization with various concentrations of [LBu- morph-AlMe2 + 2 BnOH] plotted against time with [CL] = 2.0 M in toluene 5 mL (Table S2)…………………….….................................................................................................... 8

Figure S2.	Linear plot of ln kobs against ln [LBu- morph-AlMe2 + 2 BnOH] for CL polymerization with [CL] = 2.0 M in toluene (5 mL)………………………………………………………………………………..……..…9

Table S3.	The kinetic study of polymerizations of -caprolactone using various concentrations of LCu-Nbn-AlMe2 (12) as a catalyst and BnOH as an initiator ([CL]= 2 M, toluene 5 mL, r.t.)……………………………………………........................………...…………………10

Figure S3.	First-order kinetic plots of CL polymerization with various concentrations of [LCu-Nbn-AlMe2 + 2 BnOH] plotted against time with [CL] = 2.0 M in toluene 5 mL (the first test of Table S3)……………………………………………………………………………………...…11

Figure S4.	Linear plot of ln kobs against ln [LCu-NbnAlMe2 + 2 BnOH] for CL polymerization with [CL] = 2.0 M in toluene (5 mL)…………………………………………………………………………………….….11

Table S5.	The kinetic study of polymerizations of -caprolactone using various concentrations of LCu-NOMe-AlMe2 (13) as a catalyst and BnOH as an initiator………………………....12-13

Figure S5.	First-order kinetic plots of CL polymerization with various concentrations of [LCu-NOMe-AlMe2 + 2 BnOH] plotted against time with [CL] = 2.0 M in toluene 5 mL (Table S4)……………………........................................................................................14

Figure S6.	Linear plot of ln kobs against ln [LCu-NOMeAlMe2 + 2 BnOH] for CL polymerization with [CL] = 2.0 M in toluene (5 mL)…………………………………………………………14

Figure S7-S56. 1H NMR and 13C spectra of all ligands and associated Al complexes……….……15-39

Details of the Kinetic Study of -Caprolactone Polymerization

A typical kinetic study was conducted to establish the reaction order with respect to monomer and various Al complexes. For CL polymerization, -caprolactone (1.14g, 0.01 mol) was added to a solution of the mixture of Al complexes (0.1 mmol) and BnOH (0.02 mmol) in toluene (5 mL), respectively. The solution was then stirred at room temperature under nitrogen. At the indicated time intervals, 0.05 mL aliquots were removed, trapped with CDCl3 (1mL), and analyzed by 1H NMR. The -caprolactone concentration [CL] was determined by integrating the triplet methylene peak of CL at 4.20 ppm and the triplet methylene peak of polylactone at 4.00 ppm. As expected, plots of ln([CL]0/[CL]) vs. time for a wide range of Al complexes are linear, indicating the usual first order dependence on monomer concentration (Figures S1-S2, Table S1). Thus, the rate expression can be written as -d[CL]/dt = kobs[CL]1, where kobs = kapp[Al complex + 2 BnOH]x. A plot of (kobs) vs. [Al complex + 2 BnOH] (Figure S3, Table S2) is linear, indicating the order of [Al complex + 2 BnOH] (x = 1) and kapp which is 0.296 M-1min-1.

Table S1. The kinetic study of polymerizations of -caprolactone using various Al complexes as catalysts ([CL]:[Al]:[BnOH]=100:1:2, [CL]= 2 M, toluene 5 mL, r.t.)

| Time/min | LbenAlMe2 | LesterAlMe2 | LamideAlMe2 | LBu-propAlMe2 |
| --- | --- | --- | --- | --- |
|  | Conv of PCL |
| 3 |  |  |  | 0.17 |
| 4 |  |  |  | 0.36 |
| 5 |  |  |  | 0.57 |
| 6 |  |  |  | 0.70 |
| 9 |  |  |  | 0.90 |
| 30 |  | 0.11 |  |  |
| 48 | 0.44 |  |  |  |
| 50 |  | 0.38 |  |  |
| 60 | 0.57 |  |  |  |
| 65 |  |  | 0.10 |  |
| 75 | 0.68 | 0.59 |  |  |
| 90 | 0.78 |  |  |  |
| 93 |  |  | 0.17 |  |
| 100 |  | 0.72 |  |  |
| 105 | 0.85 |  |  |  |
| 120 | 0.89 | 0.8 | 0.22 |  |
| 136 |  | 0.84 |  |  |
| 165 |  | 0.9 |  |  |
| 244 |  |  | 0.49 |  |
| 293 |  |  | 0.57 |  |
| 360 |  |  | 0.65 |  |
| 418 |  |  | 0.72 |  |
| 1020 |  |  | 0.95 |  |
| kobs × 103 | 22.8 (1) | 16.3 (2) | 3.1 (1) | 362.8 (11) |
| Induction period/min | 23 (2) | 21 (1) | 25 (7) | 3 (1) |
| R2 | 0.999 | 0.999 | 0.999 | 0.999 |

| Time/min | LAlMe2 |
| --- | --- |
|  | LH-Bu (1) | LH-py (2) | LBu-Bu (4) | LBu-morph (5) | LBu-py (6) | LMe-Py (3) | LBu-prop (8) |
|  | Conv of PCL |
| 2 |  |  |  | 0.27 |  |  |  |
| 3 |  |  |  |  | 0.16 |  | 0.17 |
| 4 |  |  |  | 0.60 |  |  | 0.36 |
| 5 |  |  |  |  |  |  | 0.57 |
| 6 |  |  |  | 0.90 | 0.41 |  | 0.70 |
| 8 |  |  |  |  |  |  |  |
| 9 |  |  |  |  | 0.60 |  | 0.90 |
| 10 |  |  | 0.13 |  |  |  |  |
| 12 |  |  |  |  | 0.73 | 0.17 |  |
| 14 |  |  |  |  |  |  |  |
| 15 |  |  |  | 0.96 | 0.82 |  |  |
| 18 |  |  |  |  | 0.90 |  |  |
| 20 | 0.36 |  | 0.34 |  |  |  |  |
| 22 |  |  |  |  |  | 0.26 |  |
| 28 | 0.46 |  |  |  |  |  |  |
| 30 |  | 0.24 | 0.5 |  |  |  |  |
| 31 |  |  |  |  |  | 0.34 |  |
| 40 | 0.56 |  | 0.64 |  |  | 0.41 |  |
| 45 |  | 0.35 |  |  |  |  |  |
| 50 |  |  | 0.73 |  |  |  |  |
| 55 |  |  |  |  |  | 0.52 |  |
| 60 |  |  | 0.80 |  |  |  |  |
| 69 |  |  |  |  |  | 0.62 |  |
| 70 | 0.72 |  |  |  |  |  |  |
| 80 |  |  | 0.91 |  |  |  |  |
| 87 |  |  |  |  |  | 0.70 |  |
| 90 | 0.81 |  |  |  |  |  |  |
| 110 | 0.87 |  |  |  |  |  |  |
| 113 |  |  |  |  |  | 0.80 |  |
| 120 | 0.90 | 0.71 |  |  |  |  |  |
| 150 |  | 0.82 |  |  |  |  |  |
| 160 |  |  |  |  |  | 0.90 |  |
| 170 |  | 0.84 |  |  |  |  |  |
| 186 |  | 0.88 |  |  |  |  |  |
| 200 |  | 0.90 |  |  |  |  |  |
| kobs × 103 | 18.2(4) | 11.7(3) | 31.9(1) | 222.5(101) | 139.5(62) | 144.3(20) | 362.8 (11) |
| Induction period/min | 3(2) | 9(3) | 7(2) | 1(1) | 2(1) | 2(1) | 3 (1) |
| R2 | 0.998 | 0.999 | 0.997 | 0.997 | 0.996 | 0.999 | 0.999 |

| Time/min | LAlMe2 |
| --- | --- |
|  | LCu-Bu (9) | LCu-py (10) | LBu-Nbn (11) | LCu-Nbn (12) | LCu-NOMe (13) | LCu-NF (14) | LCu-Nthio (15) |
|  | Conv of PCL |
| 2 |  |  |  | 0.08 |  | 0.09 | 0.10 |
| 3 |  |  | 0.31 |  |  |  |  |
| 4 |  | 0.23 | 0.46 |  |  |  |  |
| 5 | 0.13 |  | 0.54 | 0.14 | 0.11 | 0.18 | 0.18 |
| 6 |  | 0.37 |  |  |  |  |  |
| 7 |  |  | 0.76 | 0.22 |  | 0.25 | 0.20 |
| 8 |  | 0.55 |  |  |  |  |  |
| 9 |  |  | 0.88 |  |  |  |  |
| 10 | 0.20 | 0.64 |  | 0.32 | 0.16 | 0.33 | 0.31 |
| 15 |  |  |  | 0.43 | 0.25 | 0.43 | 0.40 |
| 16 |  | 0.85 |  |  |  |  |  |
| 20 | 0.29 |  |  | 0.53 |  | 0.49 | 0.45 |
| 21 |  | 0.92 |  |  |  |  |  |
| 25 |  | 0.95 |  |  |  |  |  |
| 30 | 0.38 |  |  |  | 0.48 |  |  |
| 45 |  |  |  |  | 0.67 |  |  |
| 60 | 0.65 |  |  |  | 0.76 |  |  |
| 75 |  |  |  |  | 0.86 |  |  |
| 90 | 0.83 |  |  |  |  |  |  |
| 110 | 0.89 |  |  |  |  |  |  |
| 120 |  |  |  |  | 0.95 |  |  |
| kobs × 103 | 19.6(7) | 134.0(25) | 293.7(183) | 38.2(14) | 25.5(5) | 32.1(16) | 28.3 (16) |
| Induction period/min | 3(1) | 2(1) | 2(1) | 1(1) | 2(1) | 0 | 0 |
| R2 | 0.996 | 0.999 | 0.994 | 0.997 | 0.999 | 0.995 | 0.994 |

Table S2. The kinetic study of polymerizations of -caprolactone using various concentrations of LBu- morph-AlMe2 (5) as a catalyst and BnOH as an initiator ([CL]= 2 M, toluene 5 mL, r.t.)

| Time (min) | [LBu- morph-AlMe2 + 2 BnOH] |
| --- | --- |
|  | 0.01 M | 0.015 M | 0.02 M | 0.03 M | 0.04 M |
|  | PCL conv. |
| 1 |  |  |  |  | 0.41 |
| 1.5 |  |  |  | 0.56 | 0.59 |
| 2 |  | 0.36 | 0.47 | 0.65 | 0.71 |
| 2.5 |  |  |  |  | 0.78 |
| 3 | 0.28 |  |  | 0.79 | 0.82 |
| 3.5 |  |  |  | 0.81 |  |
| 4 |  | 0.7 | 0.75 |  |  |
| 4.5 |  |  |  | 0.88 |  |
| 5 | 0.51 |  |  |  |  |
| 6 |  | 0.81 | 0.85 |  |  |
| 7 | 0.64 |  |  |  |  |
| 8 |  |  | 0.92 |  |  |
| 9 | 0.72 |  |  |  |  |
| 10 |  | 0.92 |  |  |  |
| 11 | 0.76 |  |  |  |  |
| 12 |  | 0.96 |  |  |  |
| 15 | 0.87 |  |  |  |  |
| kobs × 103 | 137.1(72) | 261.0(134) | 304.2(160) | 421.6(197) | 601.4(402) |
| Induction period/min | 0 | 0 | 0 | 0 | 0 |
| R2 | 0.986 | 0.991 | 0.998 | 0.993 | 0.992 |

Figure S1. First-order kinetic plots of CL polymerization with various concentrations of [LBu- morph-AlMe2 + 2 BnOH] plotted against time with [CL] = 2.0 M in toluene 5 mL (Table S2)

Figure S2. Linear plot of ln kobs against ln [LBu- morph-AlMe2 + 2 BnOH] for CL polymerization with [CL] = 2.0 M in toluene (5 mL)

Table S3. The kinetic study of polymerizations of -caprolactone using various concentrations of LCu-Nbn-AlMe2 (12) as a catalyst and BnOH as an initiator ([CL]= 2 M, toluene 5 mL, r.t.)

| Time (min) | [LCu-Nbn-AlMe2 + 2 BnOH] |
| --- | --- |
|  | 0.02 M | 0.03 M | 0.04 M | 0.05 M |
|  | PCL conv. |
| 2 | 0.08 | 0.09 | 0.14 | 0.19 |
| 5 | 0.14 | 0.19 | 0.27 | 0.38 |
| 7 | 0.22 | 0.30 | 0.40 | 0.53 |
| 10 | 0.32 | 0.42 | 0.52 | 0.73 |
| 15 | 0.43 | 0.56 | 0.76 | 0.83 |
| 20 | 0.53 | 0.70 | 0.84 | 0.90 |
| kobs × 103 | 38.2(14) | 62.7 (26) | 99.3(63) | 120.5(60) |
| Induction period/min | 0 | 1(1) | 2(1) | 1(1) |
| R2 | 0.997 | 0.997 | 0.992 | 0.995 |

Figure S3. First-order kinetic plots of CL polymerization with various concentrations of [LCu-Nbn-AlMe2 + 2 BnOH] plotted against time with [CL] = 2.0 M in toluene 5 mL (the first test of Table S3).

Figure S4. Linear plot of ln kobs against ln [LCu-NbnAlMe2 + 2 BnOH] for CL polymerization with [CL] = 2.0 M in toluene (5 mL)

Table S5. The kinetic study of polymerizations of -caprolactone using various concentrations of LCu-NOMe-AlMe2 (13) as a catalyst and BnOH as an initiator

| Time (min) | [LCu-NOMe-AlMe2 + 2 BnOH] |
| --- | --- |
|  | 0.02 M | 0.03 M | 0.04 M | 0.05 M |
|  | PCL conv. |
| 2 |  | 0.11 | 0.17 | 0.18 |
| 4 |  |  |  | 0.28 |
| 5 | 0.11 | 0.21 | 0.26 |  |
| 6 |  |  |  | 0.41 |
| 7 |  | 0.30 |  |  |
| 8 |  |  |  | 0.50 |
| 10 | 0.16 | 0.42 | 0.45 | 0.55 |
| 15 | 0.25 | 0.46 | 0.62 | 0.70 |
| 20 |  | 0.57 | 0.72 | 0.78 |
| 25 |  |  | 0.80 |  |
| 30 | 0.48 | 0.75 |  |  |
| 45 | 0.67 |  |  |  |
| 60 | 0.76 |  |  |  |
| 75 | 0.86 |  |  |  |
| 120 | 0.95 |  |  |  |
| kobs × 103 | 25.8(6) | 43.6 (25) | 63.3(19) | 68.0(29) |
| Induction period/min | 3(1) | 0 | 0 | 1(1) |
| R2 | 0.999 | 0.992 | 0.998 | 0.995 |

Figure S5. First-order kinetic plots of CL polymerization with various concentrations of [LCu-NOMe-AlMe2 + 2 BnOH] plotted against time with [CL] = 2.0 M in toluene 5 mL (Table S4).

Figure S6. Linear plot of ln kobs against ln [LCu-NOMeAlMe2 + 2 BnOH] for CL polymerization with [CL] = 2.0 M in toluene (5 mL)

Figure S7. 1H NMR spectrum of Lamide-H

Figure S8. 13C NMR spectrum of Lamide-H

Figure S9. 1H NMR spectrum of Lester-H

Figure S10. 13C NMR spectrum of Lester-H

Figure S11. 1H NMR spectrum of LPh-Bu-H

Figure S12. 13C NMR spectrum of LPh-Bu-H

Figure S13. 1H NMR spectrum of LPh-py-H

Figure S14. 13C NMR spectrum of LPh-py-H

Figure S15. 1H NMR spectrum of LBu-Nbn-H

Figure S16. 13C NMR spectrum of LBu-Nbn-H

Figure S17. 1H NMR spectrum of LPh-Nbn-H

Figure S18. 13C NMR spectrum of LPh-Nbn-H

Figure S19. 1H NMR spectrum of LPh-NOMe-H

Figure S20. 13C NMR spectrum of LPh-NOMe-H

Figure S20. 1H NMR spectrum of LPh-NF-H

Figure S22. 13C NMR spectrum of LPh-NF-H

Figure S23. 1H NMR spectrum of LPh-thio-H

Figure S24. 13C NMR spectrum of LPh-thio-H

Figure S25. 1H NMR spectrum of Lamide-AlMe2

Figure S26. 13C NMR spectrum of Lamide-AlMe2

Figure S27. 1H NMR spectrum of Lamide-AlsioBu2

Figure S28. 13C NMR spectrum of Lamide-AlsioBu2

Figure S29. 1H NMR spectrum of Lester-AlMe2

Figure S30. 13C NMR spectrum of Lester-AlMe2

Figure S31. 1H NMR spectrum of LH-Bu-AlMe2

Figure S32. 13C NMR spectrum of LH-Bu-AlMe2

Figure S33. 1H NMR spectrum of LH-py-AlMe2

Figure S34. 13C NMR spectrum of LH-py-AlMe2

Figure S35. 1H NMR spectrum of LBu-Bu-AlMe2

Figure S36. 13C NMR spectrum of LBu-Bu-AlMe2

Figure S37. 1H NMR spectrum of LBu-morph-AlMe2

Figure S38. 13C NMR spectrum of LBu-morph-AlMe2

Figure S39. 1H NMR spectrum of LBu-Cy-AlMe2

Figure S40. 13C NMR spectrum of LBu-Cy-AlMe2

Figure S41. 1H NMR spectrum of LBu-prop-AlMe2

Figure S42. 13C NMR spectrum of LBu-prop-AlMe2

Figure S43. 1H NMR spectrum of LBu-NBn-AlMe2

Figure S44. 13C NMR spectrum of LBu-NBn-AlMe2

Figure S45. 1H NMR spectrum of LCu-Bu-AlMe2

Figure S46. 13C NMR spectrum of LCu-Bu-AlMe2

Figure S47. 1H NMR spectrum of LCu-py-AlMe2

Figure S48. 13C NMR spectrum of LCu-py-AlMe2

Figure S49. 1H NMR spectrum of LCu-Nbn-AlMe2

Figure S50. 13C NMR spectrum of LCu-Nbn-AlMe2

Figure S51. 1H NMR spectrum of LCu-NOMe-AlMe2

Figure S52. 13C NMR spectrum of LCu-NOMe-AlMe2

Figure S53. 1H NMR spectrum of LCu-NF-AlMe2

Figure S54. 13C NMR spectrum of LCu-NF-AlMe2

Figure S55. 1H NMR spectrum of LCu-Nthio-AlMe2

Figure S56. 13C NMR spectrum of LCu-Nthio-AlMe2