Supporting information

Branched polyethylenes using thermally enhanced bis(imino)acenaphthene- nickel catalysts: exploring the effects of temperature and pressure

Qiuyue Zhang,a,b Randi Zhang,a,b Yanping Ma,a,b Gregory A. Solan,*a,c Tongling Lianga and Wen-Hua Suna,b,d*

a Key Laboratory of Engineering Plastics and Beijing National Laboratory for Molecular Sciences, Institute of Chemistry, Chinese Academy of Sciences, Beijing 100190, China.

b CAS Research/Education Center for Excellence in Molecular Sciences, University of Chinese Academy of Sciences, Beijing 100049, China.

c Department of Chemistry, University of Leicester, University Road, Leicester LE1 7RH, UK.

d State Key Laboratory for Oxo Synthesis and Selective Oxidation, Lanzhou Institute of Chemical Physics, Chinese Academy of Sciences, Lanzhou 730000, China.

Contents

- 13C NMR spectra of the polyethylenes and their interpretation

- Figure S1 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 30 °C under 10 atm ethylene (entry 2, Table 6).

- Figure S2 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 70 °C under 10 atm ethylene (entry 9, Table 6).

- Figure S3 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 90 °C under 10 atm ethylene (entry 10, Table 6).

- Figure S4 13C NMR spectrum of the polyethylene obtained using Ni5/MAO at 90 °C under 10 atm ethylene (entry 10, Table 4).

- Figure S5 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 30 °C under 1 atm ethylene (entry 3, Table 5).

- Figure S6 Elastic recovery curves for PE-70E/10atm at -10 and 30 °C (10 cycles).

- Figure S7 1H NMR spectra of Ni1 – Ni5 (recorded in CDCl3 at ambient temperature)

- Table S1 Branching analysis of PE-30M/10atm obtained using Ni5/MAO at 30 °C under 10 atm ethylene

- Table S2 Branching analysis of PE-70M/10atm obtained using Ni5/MAO at 70 °C under 10 atm ethylene

- Table S3 Branching analysis of PE-90M10atm obtained using Ni5/MAO at 90 °C under 10 atm ethylene

- Table S4 Branching analysis of PE-30M/1atm obtained using Ni5/MAO at 30 °C under 1 atm ethylene

- Table S5 Branching analysis of PE-30E/10atm obtained using Ni5/EASC at 30 °C under 10 atm ethylene

- Table S6 Branching analysis of PE-70E/10 atm obtained using Ni5/EASC at 70 °C under 10 atm ethylene

- Table S7 Branching analysis of PE-90E/10atm obtained using Ni5/EASC at 90 °C under 10 atm ethylene

- Table S8 Branching analysis of PE-30E/1atm obtained using Ni5/EASC at 30 °C under 1 atm ethylene

- Table S9 Crystal data and structure refinements for Ni3 and Ni7.

13C NMR spectra of the polyethylenes and their interpretation

For the 13C NMR spectra of the polyethylenes, a weighed amount of polyethylene (80 - 100 mg) was dissolved in 1,1,2,2-tetrachloroethane-d2 (2 mL) with TMS as an internal standard and inverse gated 13C spectra recorded on a Bruker DMX 300 spectrometer at 75.47 MHz in 5 mm standard glass tubes at 100 °C with the number of scans between 2000 and 3000. Operating conditions used: spectral width 17.9856 kHz; acquisition time 1.8219 s; relaxation delay 2.0 s.

An estimation of the branching content was made by integration of the corresponding peaks in the 13C NMR spectra using approaches described in the literature [G. B. Galland, R. Quijada, R. Rojas, G. Bazan, Z. J. A. Komon, NMR Study of Branched Polyethylenes Obtained with Combined Fe and Zr Catalysts, Macromolecules 35 (2002) 339-345].

Figure S1 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 30 °C under 10 atm ethylene (entry 2, Table 6).

Figure S2 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 70 °C under 10 atm ethylene (entry 9, Table 6).

Figure S3 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 90 °C under 10 atm ethylene (entry 10, Table 6).

Figure S4 13C NMR spectrum of the polyethylene obtained using Ni5/MAO at 90 °C under 10 atm ethylene (entry 10, Table 4).

Figure S5 13C NMR spectrum of the polyethylene obtained using Ni5/EASC at 30 °C under 1 atm ethylene (entry 3, Table 5).

Figure S6 Elastic recovery curves for PE-70E/10atm at -10 and 30 °C (10 cycles).

Figure S7 1H NMR spectra of Ni1 – Ni5 (recorded in CDCl3 at ambient temperature)

| Table S1 Branching analysis of PE-30M/10atm obtained using Ni5/MAO at 30 °C under 10 atm ethylenea |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.22 | NM | 4.6 | 56.78% |
| 2 | 14.27 | 1 | NE | 0.16 | 2.00% |
| 3 | 14.77 | 0.18 | NP | 0.27 | 3.36% |
| 4 | 19.86 | 0.17 | NB | 0.53 | 6.48% |
| 5 | 20.12 | 2.39 | NA | 0.38 | 4.69% |
| 6 | 20.33 | 1.13 | NM(1,4) | 0.81 | 9.94% |
| 7 | 22.93 | 0.57 | NM(1,5) | 0 | 0 |
| 8 | 23.42 | 0.1 | NM(1,6) | 0.53 | 6.54% |
| 9 | 24.67 | 0 | NL | 0.49 | 5.99% |
| 10 | 26.69 | 0.12 | NL(1,4) | 0.35 | 4.26% |
| 11 | 27.25 | 2.2 |  |  |  |
| 12 | 27.44 | 5.86 | [E] | 17.65 |  |
| 13 | 27.83 | 1.06 | [R] | 8.10 |  |
| 14 | 29.53 | 0.22 |  |  |  |
| 15 | 29.61 | 0.62 | Total | 157.30 |  |
| 16 | 30 | 36.31 | branching | Branches/1000C |  |
| 17 | 30.38 | 9.42 |  |  |  |
| 18 | 30.48 | 1.57 | Methyl branches |  | 73.22% |
| 19 | 31.68 | 0.72 | Ethyl branches |  | 2.00% |
| 20 | 32.23 | 1.01 | Propyl branches |  | 3.36% |
| 21 | 32.72 | 0.38 | Butyl branches |  | 6.48% |
| 22 | 33.22 | 2.3 | Amyl branches |  | 4.69% |
| 23 | 33.57 | 1.1 | Longer branches |  | 10.25% |
| 24 | 33.83 | 0.11 |  |  |  |
| 25 | 34.01 | 0.95 |  |  |  |
| 26 | 34.49 | 3.1 |  |  |  |
| 27 | 34.86 | 1.06 |  |  |  |
| 28 | 36.94 | 0.27 |  |  |  |
| 29 | 37.55 | 5.03 |  |  |  |
| 30 | 37.86 | 0.51 |  |  |  |
| 31 | 38.1 | 1.21 |  |  |  |
| 32 | 38.37 | 0.33 |  |  |  |
| 33 | 39.62 | 0.31 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S2 Branching analysis of PE-70M/10atm obtained using Ni5/MAO at 70 °C under 10 atm ethylenea |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.4 | NM | 1.69 | 31.43% |
| 2 | 14.27 | 1 | NE | 0.35 | 6.51% |
| 3 | 14.77 | 0.29 | NP | 0.44 | 8.18% |
| 4 | 19.86 | 0.11 | NB | 0.450 | 9.21% |
| 5 | 20.12 | 2.57 | NA | 0.35 | 6.51% |
| 6 | 20.33 | 0.2 | NM(1,4) | 0.69 | 12.88% |
| 7 | 22.93 | 0.76 | NM(1,5) | 0.15 | 2.79% |
| 8 | 23.42 | 0.3 | NM(1,6) | 0.55 | 10.13% |
| 9 | 24.67 | 0.15 | NL | 0.28 | 5.11% |
| 10 | 26.69 | 0.43 | NL(1,4) | 0.39 | 7.25% |
| 11 | 27.25 | 1.3 |  |  |  |
| 12 | 27.44 | 3.01 | [E] | 5.49 |  |
| 13 | 27.83 | 1.09 | [R] | 5.38 |  |
| 14 | 29.53 | 0.1 |  |  |  |
| 15 | 29.61 | 1.38 | Total | 247.53 |  |
| 16 | 30 | 11.75 | branching | Branches/1000 Cs |  |
| 17 | 30.38 | 6.66 |  |  |  |
| 18 | 30.48 | 0.65 | Methyl branches |  | 57.23% |
| 19 | 31.68 | 0.46 | Ethyl branches |  | 6.51% |
| 20 | 32.23 | 0.78 | Propyl branches |  | 8.18% |
| 21 | 32.72 | 0.35 | Butyl branches |  | 9.21% |
| 22 | 33.22 | 1.16 | Amyl branches |  | 6.51% |
| 23 | 33.57 | 0.83 | Longer branches |  | 12.36% |
| 24 | 33.83 | 0.52 |  |  |  |
| 25 | 34.01 | 0.69 |  |  |  |
| 26 | 34.49 | 2.13 |  |  |  |
| 27 | 34.86 | 0.97 |  |  |  |
| 28 | 36.94 | 0.44 |  |  |  |
| 29 | 37.55 | 2.93 |  |  |  |
| 30 | 37.86 | 0.56 |  |  |  |
| 31 | 38.1 | 0.73 |  |  |  |
| 32 | 38.37 | 0.55 |  |  |  |
| 33 | 39.62 | 0.36 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S3 Branching analysis of PE-90M10atm obtained using Ni5/MAO at 90 °C under 10 atm ethylenea |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.44 | NM | 0.97 | 22.83% |
| 2 | 14.27 | 1 | NE | 0.34 | 8.00% |
| 3 | 14.77 | 0.17 | NP | 0.33 | 7.76% |
| 4 | 19.86 | 0.18 | NB | 0.51 | 11.88% |
| 5 | 20.12 | 1.84 | NA | 0.18 | 4.24% |
| 6 | 20.33 | 0.45 | NM(1,4) | 0.55 | 12.94% |
| 7 | 22.93 | 0.83 | NM(1,5) | 0.25 | 5.88% |
| 8 | 23.42 | 0.35 | NM(1,6) | 0.59 | 13.88% |
| 9 | 24.67 | 0.25 | NL | 0.36 | 8.35% |
| 10 | 26.69 | 0.88 | NL(1,4) | 0.18 | 4.24% |
| 11 | 27.25 | 2.16 |  |  |  |
| 12 | 27.44 | 2.27 | [E] | 3.92 |  |
| 13 | 27.83 | 1.18 | [R] | 4.25 |  |
| 14 | 29.53 | 0 |  |  |  |
| 15 | 29.61 | 1.5 | Total | 260.10 |  |
| 16 | 30 | 8.43 | branching | Branches/1000C |  |
| 17 | 30.38 | 1.93 |  |  |  |
| 18 | 30.48 | 1.86 | Methyl branches |  | 55.53% |
| 19 | 31.68 | 0.22 | Ethyl branches |  | 8.00% |
| 20 | 32.23 | 0.59 | Propyl branches |  | 7.76% |
| 21 | 32.72 | 0.18 | Butyl branches |  | 11.88% |
| 22 | 33.22 | 1.01 | Amyl branches |  | 4.24% |
| 23 | 33.57 | 0.76 | Longer branches |  | 12.59% |
| 24 | 33.83 | 0 |  |  |  |
| 25 | 34.01 | 0.66 |  |  |  |
| 26 | 34.49 | 1.89 |  |  |  |
| 27 | 34.86 | 0.72 |  |  |  |
| 28 | 36.94 | 0.33 |  |  |  |
| 29 | 37.55 | 2.45 |  |  |  |
| 30 | 37.86 | 0.16 |  |  |  |
| 31 | 38.1 | 0.94 |  |  |  |
| 32 | 38.37 | 0.25 |  |  |  |
| 33 | 39.62 | 0.14 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S4 Branching analysis of PE-30M/1atm obtained using Ni5/MAO at 30 °C under 1 atm ethylene a |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.26 | NM | 0.94 | 31.00% |
| 2 | 14.27 | 1 | NE | 0.17 | 5.60% |
| 3 | 14.77 | 0.14 | NP | 0.18 | 5.93% |
| 4 | 19.86 | 0.18 | NB | 0.36 | 11.71% |
| 5 | 20.12 | 1.66 | NA | 0.06 | 1.98% |
| 6 | 20.33 | 0.31 | NM(1,4) | 0.39 | 12.78% |
| 7 | 22.93 | 0.77 | NM(1,5) | 0.14 | 4.62% |
| 8 | 23.42 | 0.21 | NM(1,6) | 0.34 | 11.05% |
| 9 | 24.67 | 0.14 | NL | 0.4 | 13.19% |
| 10 | 26.69 | 0.41 | NL(1,4) | 0.07 | 2.14% |
| 11 | 27.25 | 2.07 |  |  |  |
| 12 | 27.44 | 1.71 | [E] | 3.55 |  |
| 13 | 27.83 | 0.67 | [R] | 3.03 |  |
| 14 | 29.53 | 0.28 |  |  |  |
| 15 | 29.61 | 1.11 | Total | 230.52 |  |
| 16 | 30 | 7.58 | branching | Branches/1000C |  |
| 17 | 30.38 | 1.37 |  |  |  |
| 18 | 30.48 | 1.47 | Methyl branches |  | 57.45% |
| 19 | 31.68 | 0.1 | Ethyl branches |  | 5.60% |
| 20 | 32.23 | 0.49 | Propyl branches |  | 5.93% |
| 21 | 32.72 | 0.06 | Butyl branches |  | 11.71% |
| 22 | 33.22 | 0.88 | Amyl branches |  | 1.98% |
| 23 | 33.57 | 0.57 | Longer branches |  | 15.33% |
| 24 | 33.83 | 0.12 |  |  |  |
| 25 | 34.01 | 0.5 |  |  |  |
| 26 | 34.49 | 1.92 |  |  |  |
| 27 | 34.86 | 0.49 |  |  |  |
| 28 | 36.94 | 0.18 |  |  |  |
| 29 | 37.55 | 2.1 |  |  |  |
| 30 | 37.86 | 0.08 |  |  |  |
| 31 | 38.1 | 0.48 |  |  |  |
| 32 | 38.37 | 0.08 |  |  |  |
| 33 | 39.62 | 0.04 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S5 Branching analysis of PE-30E/10atm obtained using Ni5/EASC at 30 °C under 10 atm ethylene a |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.13 | NM | 3.12 | 42.77% |
| 2 | 14.27 | 1 | NE | 0.21 | 2.86% |
| 3 | 14.77 | 0.12 | NP | 0.43 | 5.90% |
| 4 | 19.86 | 0.11 | NB | 0.54 | 7.41% |
| 5 | 20.12 | 3.03 | NA | 0.53 | 7.28% |
| 6 | 20.33 | 0.38 | NM(1,4) | 0.915 | 12.56% |
| 7 | 22.93 | 0.75 | NM(1,5) | 0 | 0% |
| 8 | 23.42 | 0.02 | NM(1,6) | 0.495 | 6.80% |
| 9 | 24.67 | 0 | NL | 0.535 | 7.35% |
| 10 | 26.69 | 0.15 | NL(1,4) | 0.515 | 7.07% |
| 11 | 27.25 | 2.63 |  |  |  |
| 12 | 27.44 | 4.47 | [E] | 17.58 |  |
| 13 | 27.83 | 0.99 | [R] | 7.28 |  |
| 14 | 29.53 | 0.22 |  |  |  |
| 15 | 29.61 | 1.03 | Total | 146.48 |  |
| 16 | 30 | 36.38 | branching | Branches/1000C |  |
| 17 | 30.38 | 13.69 |  |  |  |
| 18 | 30.48 | 0.85 | Methyl branches |  | 62.13% |
| 19 | 31.68 | 0.68 | Ethyl branches |  | 2.86% |
| 20 | 32.23 | 1.22 | Propyl branches |  | 5.90% |
| 21 | 32.72 | 0.53 | Butyl branches |  | 7.41% |
| 22 | 33.22 | 2.29 | Amyl branches |  | 7.28% |
| 23 | 33.57 | 1.1 | Longer branches |  | 14.42% |
| 24 | 33.83 | 0.11 |  |  |  |
| 25 | 34.01 | 1.06 |  |  |  |
| 26 | 34.49 | 3.33 |  |  |  |
| 27 | 34.86 | 1.28 |  |  |  |
| 28 | 36.94 | 0.43 |  |  |  |
| 29 | 37.55 | 5.15 |  |  |  |
| 30 | 37.86 | 0.94 |  |  |  |
| 31 | 38.1 | 1.28 |  |  |  |
| 32 | 38.37 | 0.69 |  |  |  |
| 33 | 39.62 | 0.42 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S6 Branching analysis of PE-70E/10 atm obtained using Ni5/EASC at 70 °C under 10 atm ethylene a |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.15 | NM | 1.23 | 28.11% |
| 2 | 14.27 | 1 | NE | 0.11 | 2.51% |
| 3 | 14.77 | 0.19 | NP | 0.21 | 4.79% |
| 4 | 19.86 | 0.05 | NB | 0.44 | 9.92% |
| 5 | 20.12 | 1.86 | NA | 0.31 | 7.07% |
| 6 | 20.33 | 0.26 | NM(1,4) | 0.76 | 17.33% |
| 7 | 22.93 | 0.71 | NM(1,5) | 0.1 | 2.28% |
| 8 | 23.42 | 0.15 | NM(1,6) | 0.46 | 10.38% |
| 9 | 24.67 | 0.1 | NL | 0.36 | 8.10% |
| 10 | 26.69 | 0.05 | NL(1,4) | 0.42 | 9.51% |
| 11 | 27.25 | 1.65 |  |  |  |
| 12 | 27.44 | 2.43 | [E] | 5.48 |  |
| 13 | 27.83 | 0.91 | [R] | 4.39 |  |
| 14 | 29.53 | 0.12 |  |  |  |
| 15 | 29.61 | 0.44 | Total | 222.36 |  |
| 16 | 30 | 11.87 | branching | Branches/1000C |  |
| 17 | 30.38 | 6.22 |  |  |  |
| 18 | 30.48 | 0.96 | Methyl branches |  | 58.1% |
| 19 | 31.68 | 0.59 | Ethyl branches |  | 2.51% |
| 20 | 32.23 | 0.92 | Propyl branches |  | 4.79% |
| 21 | 32.72 | 0.31 | Butyl branches |  | 9.92% |
| 22 | 33.22 | 1.11 | Amyl branches |  | 7.07% |
| 23 | 33.57 | 0.86 | Longer branches |  | 17.61% |
| 24 | 33.83 | 0 |  |  |  |
| 25 | 34.01 | 0.72 |  |  |  |
| 26 | 34.49 | 2.7 |  |  |  |
| 27 | 34.86 | 1.09 |  |  |  |
| 28 | 36.94 | 0.21 |  |  |  |
| 29 | 37.55 | 2.68 |  |  |  |
| 30 | 37.86 | 0.11 |  |  |  |
| 31 | 38.1 | 1.11 |  |  |  |
| 32 | 38.37 | 0.54 |  |  |  |
| 33 | 39.62 | 0.28 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S7 Branching analysis of PE-90E/10atm obtained using Ni5/EASC at 90 °C under 10 atm ethylene a |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.31 | NM | 0.50 | 15.51 |
| 2 | 14.27 | 1 | NE | 0.25 | 7.94 |
| 3 | 14.77 | 0.17 | NP | 0.21 | 6.58 |
| 4 | 19.86 | 0.18 | NB | 0.42 | 13.16 |
| 5 | 20.12 | 1.68 | NA | 0.12 | 3.76 |
| 6 | 20.33 | 0.2 | NM(1,4) | 0.44 | 13.71 |
| 7 | 22.93 | 0.85 | NM(1,5) | 0.20 | 6.27 |
| 8 | 23.42 | 0.22 | NM(1,6) | 0.50 | 15.67 |
| 9 | 24.67 | 0.2 | NL | 0.44 | 13.79 |
| 10 | 26.69 | 0.66 | NL(1,4) | 0.12 | 3.61 |
| 11 | 27.25 | 2.12 |  |  |  |
| 12 | 27.44 | 1.54 | [E] | 3.78 |  |
| 13 | 27.83 | 1 | [R] | 3.19 |  |
| 14 | 29.53 | 0 |  |  |  |
| 15 | 29.61 | 1.07 | Total | 229.03 |  |
| 16 | 30 | 8.14 | branching | Branches/1000C |  |
| 17 | 30.38 | 1.54 |  |  |  |
| 18 | 30.48 | 1.7 | Methyl branches |  | 51.16% |
| 19 | 31.68 | 0.14 | Ethyl branches |  | 7.94% |
| 20 | 32.23 | 0.59 | Propyl branches |  | 6.58% |
| 21 | 32.72 | 0.12 | Butyl branches |  | 13.16% |
| 22 | 33.22 | 0.9 | Amyl branches |  | 3.76% |
| 23 | 33.57 | 0.53 | Longer branches |  | 17.40% |
| 24 | 33.83 | 0 |  |  |  |
| 25 | 34.01 | 0.62 |  |  |  |
| 26 | 34.49 | 2.02 |  |  |  |
| 27 | 34.86 | 0.61 |  |  |  |
| 28 | 36.94 | 0.21 |  |  |  |
| 29 | 37.55 | 2.13 |  |  |  |
| 30 | 37.86 | 0.16 |  |  |  |
| 31 | 38.1 | 0.58 |  |  |  |
| 32 | 38.37 | 0.16 |  |  |  |
| 33 | 39.62 | 0.1 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S8 Branching analysis of PE-30E/1atm obtained using Ni5/EASC at 30 °C under 1 atm ethylene a |
| --- |
| Peak no. |  (ppm) | Relative integral | Type of branch |  | Relative percentage of branch |
| 1 | 11.31 | 0.2 | NM | 0.74 | 27.90% |
| 2 | 14.27 | 1 | NE | 0.19 | 7.28% |
| 3 | 14.77 | 0.11 | NP | 0.11 | 4.18% |
| 4 | 19.86 | 0.13 | NB | 0.29 | 11.01% |
| 5 | 20.12 | 1.69 | NA | 0.04 | 1.52% |
| 6 | 20.33 | 0.2 | NM(1,4) | 0.24 | 9.02% |
| 7 | 22.93 | 0.84 | NM(1,5) | 0.2 | 7.59% |
| 8 | 23.42 | 0.2 | NM(1,6) | 0.34 | 12.91% |
| 9 | 24.67 | 0.2 | NL | 0.46 | 17.27% |
| 10 | 26.69 | 0.24 | NL(1,4) | 0.04 | 1.32% |
| 11 | 27.25 | 1.72 |  |  |  |
| 12 | 27.44 | 1.46 | [E] | 4.16 |  |
| 13 | 27.83 | 0.68 | [R] | 2.63 |  |
| 14 | 29.53 | 0.51 |  |  |  |
| 15 | 29.61 | 1.47 | Total | 194.00 |  |
| 16 | 30 | 8.81 | branching | Branches/1000C |  |
| 17 | 30.38 | 1.75 |  |  |  |
| 18 | 30.48 | 1 | Methyl branches |  | 57.42% |
| 19 | 31.68 | 0.04 | Ethyl branches |  | 7.28% |
| 20 | 32.23 | 0.5 | Propyl branches |  | 4.18% |
| 21 | 32.72 | 0.04 | Butyl branches |  | 11.01% |
| 22 | 33.22 | 0.71 | Amyl branches |  | 1.52% |
| 23 | 33.57 | 0.37 | Longer branches |  | 18.59% |
| 24 | 33.83 | 0.53 |  |  |  |
| 25 | 34.01 | 0.38 |  |  |  |
| 26 | 34.49 | 1.9 |  |  |  |
| 27 | 34.86 | 0.29 |  |  |  |
| 28 | 36.94 | 0.11 |  |  |  |
| 29 | 37.55 | 1.81 |  |  |  |
| 30 | 37.86 | 0.11 |  |  |  |
| 31 | 38.1 | 0.52 |  |  |  |
| 32 | 38.37 | 0.05 |  |  |  |
| 33 | 39.62 | 0.07 |  |  |  |
| a Data determined from the 13C NMR spectrum using approaches described by G. B. Galland, R. F. de Souza, R. S. Mauler and F. F. Nunes, Macromolecules, 1999, 32, 1620-1625. |

| Table S9 Crystal data and structure refinements for Ni3 and Ni7 |
| --- |
|  | Ni3 | Ni7 |
| CCDC No. Empirical formula | 1854203 C60H52Br2F4N2Ni·2CH2Cl2 | 1854204 C58H48Cl2F4N2Ni·(C2H5)2O |
| Formula weight | 1265.45 | 1052.71 |
| Temperature/K | 173.15 | 173.1500 |
| Crystal system | triclinic | monoclinic |
| Space group | P1 | P21 |
| a/Å | 10.598(2) | 10.479(2) |
| b/Å | 11.685(2) | 19.556(4) |
| c/Å | 13.282(3) | 13.067(3) |
| α/° | 75.04(3) | 90 |
| β/° | 84.64(3) | 93.20(3) |
| γ/° | 64.83(3) | 90 |
| Volume/Å3 | 1437.9(6) | 2673.6(9) |
| Z | 1 | 2 |
| ρcalcg/cm3 | 1.4612 | 1.308 |
| μ/mm-1 | 1.966 | 0.520 |
| F(000) | 644.6 | 1100.0 |
| Crystal size/mm3 | 0.453 × 0.147 × 0.041 | 0.229 × 0.176 × 0.048 |
| 2Θ range for data collection/° | 4.24 to 50 | 3.122 to 55.044 |
| Index ranges | -13 ≤ h ≤ 13, -15 ≤ k ≤ 15, -17 ≤ l ≤ 17 | -13 ≤ h ≤ 13, -25 ≤ k ≤ 24, -16 ≤ l ≤ 16 |
| Reflections collected | 15146 | 21234 |
| Independent reflections | 8963 [Rint = 0.0420, Rsigma = 0.0554] | 11869 [Rint = 0.0432, Rsigma = 0.0647] |
| Data/restraints/parameters | 8963/49/703 | 11869/143/714 |
| Goodness-of-fit on F2 | 1.046 | 1.044 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0662, wR2 = 0.1807 | R1 = 0.0614, wR2 = 0.1449 |
| Final R indexes [all data] | R1 = 0.0674, wR2 = 0.1827 | R1 = 0.0662, wR2 = 0.1505 |
| Largest diff. peak/hole / e Å-3 | 0.92/-0.60 | 1.00/-0.43 |
| Flack parameter | 0.139(13) | 0.036(19) |