Supporting Information

# Self-Floating Bi2S3/Poly (vinylidene fluoride) Composites Based on Polyurethane Sponges for Highly Efficient Solar Water Purification

Haiyan Cheng, Xinghang Liu, Lixing Zhang, Fang Yu, Baofei Hou, ZhuoXun Shi and Xianbao Wang*

Hubei Collaborative Innovation Center for Advanced Organic Chemical Materials, Ministry-of-Education Key Laboratory for the Green Preparation and Application of Functional Materials, Hubei Key Laboratory of Polymer Materials (Hubei University), School of Materials Science and Engineering, Hubei University. Wuhan 430062, P. R. China.

* Corresponding author. Tel.: +86 27 88661729; fax: +86 27 88661729.

E-mail addresses: wangxb68@aliyun.com (Xianbao Wang)

Preparation of MP and PBP-Rx.

Determination of optimum dosage of PVDF.

In order to realize the high efficiency of solar water purification (SWP), it’s necessary to design PP in an appropriate way, to promote the water transport without impacting the utilization of incident light. The effect of PVDF’s dosage on SWP was studied. The mass percent of 4, 8, 10, 12, 14, 16 wt% PVDF (to DMF) were selected to prepare PP composites. Fig. S2 shows the optical images and images of their floating states. It could be obviously observed that, as the dosage of PVDF increased, opaque white gels accumulated at the surface of PP, which would impair light harvest. While less dosage of PVDF would damage the mechanical property of PP. Consequently, we selected 8 wt% PVDF (to DMF) as the optimum dosage of PVDF to prepare PP composites.

Determination of the optimum thickness of PU.

Heat management and water transport are both important for SWP. So an appropriate floating state will facilitate the evaporative capability. Here, when the thickness of BP is constant, the floating states of PP samples with different thickness of PU were investigated. As shown in Fig. S3, it’s easy to sink to the bottom of the beaker, when the sample was too thin to maintain the floating state (Fig. S3a), thus weakening the heat management. While sample c (Fig. S3c) was too thick to satisfy water supply (Fig. S3c). Here we selected 10 mm as the optimum thickness of PU to prepare PP composites.

Determination of the optimum dosage of Bi2S3.

In order to realize the high efficiency and high stability of SWP device, it’s necessary to investigate the optimum dosage of Bi2S3 to prepare PBP-Rx composites. The amount of 1, 3, 5, 7, 9 mg/mL Bi2S3 (to the volume of DMF) were selected to prepare PBP-R1.5 composites. And we measured the mass change through water evaporation enabled by these composites with different dosage of Bi2S3 under 1 sun illumination. As displayed in Fig. S4a, all composites doped with Bi2S3 exhibited higher mass change. Besides, with the increase of the amount of Bi2S3, the amount of solar steam generated increased. But when the dosage of Bi2S3 was higher than 5mg/mL, some black objects shedding was observed in Fig. S4b, couldn’t well satisfy the requirement of high stability. So we selected 5 mg/mL Bi2S3 (to the volume of DMF) to prepare PBP-Rx composites.

Fabrication of chrysanthemum-like Bi2S3.

Mechanical and chemical stability of PBP-R1.5.

Table S1 The properties of polyurethane (PU) sponges.

| Bore diameter (μm) | Hardness （Asker）（°） | Elongation % | tensile strength Kg/cm2 | Tear strength Kg/cm | Bulk density Kg/m3 |
| --- | --- | --- | --- | --- | --- |
| 60±5 | 65-80 | 0.5 | 1.5 | 80 | 22±2 |

* The data was provided by manufacturers of PU sponges.

Table S2. Essential parameters for different SWP system. (1 Sun=1 kW m-2)

| Materials | system | Power density kW m-2 | Evaporation rate | Efficiency % | Refs. |
| --- | --- | --- | --- | --- | --- |
| Oligoaniline foam/PHTs | Floating system | 1 | 1.1687 kg m-2 h-1 | 80.5 | [1] |
| Activated carbon fiber | Floating system | 1 | 1.22 kg m-2 h-1 | 79.4 | [2] |
| rGO/MCE membrane-PU | Floating system | 1 | 0.838 kg m-2 h-1 | ~60 | [3] |
| PU sponges | Floating system | 1 | 0.83 kg m-2 h-1 | ~52.2 | [4] |
| rGO/PU foam | Floating system | 1 | 0.9 kg m-2 h-1 | 65 | [5] |
| F-wood/CNTs | Floating system | 1 | 0.95 kg m-2 h-1 | 65 | [6] |
| RGO/BNC:BNC aerogel | Floating system | 10 | 11.8 kg m-2 h-1 |  | [7] |
| Carbon black | Suspending system | 10 |  | 69 | [8] |
| Hollow carbon beads | Floating system | 1 | 1.28 L m−2 h−1 |  | [9] |
| Flame-treated wood | Floating system | 1 |  | ~72 | [10] |
| Carbonized mushroom | Floating system | 1 | 1.475 | ~78 | [11] |
| Carbon Sponges | Floating system | 1 | 1.39 kg m-2 h-1 | 90 | [12] |
| rGO nanofluids | Suspending system | 1 | 0.9 kg m-2 h-1 | ~47 | [13] |
| SiO2/Ag@TiO2 core–shell | Suspending system | 1 | 5.68 | 70.8 | [14] |
| Au nanofluids | Suspending system | 220 |  | 80.3 | [15] |
| 3D printed CNT/GO | Floating system | 1 | 1.25 | 85.6 | [16] |
| Carbonized rice straw-bacterial cellulose/culms | Floating system | 1 | 1.2 kg m-2 h-1 | 75.8 | [17] |
| Carbon fibers | Floating system | 1 | 1.47 | 92.5 | [19] |
| Aluminium nanoparticles | Floating system | 4 | 5.7 | 88.4 | [22] |
| Ti3C2 membrane | Floating system |  | 1.33 | 84 | [23] |
| Bi2S3/PVDF-PU sponges | Floating system | 1 | 1.66 kg m-2 h-1 | 92.9 | Our work |

The analysis of heat loss[11][18][19].

- Radiation:

The radiation heat flux was calculated based on the Stefan-Boltzmann Equation:

Φ=εAσ(T14-T24)                                                   (1)

Where Φ (W m-2) is the radiation heat flux; ε is the emissivity of samples, that’s 0.97 (estimated based on Kirchhoff Law[20], ε=α, α-absorbility, Note S); A (m2) is the surface area (D46 mm); σ is the Stefan-Boltzmann constant, that’s 5.67×10-8 W m-2 K-4; T1 is the average surface temperature (≈43.6 °C) of samples at a steady state under 1 sun irradiation, T2 is the temperature (≈42 °C) of steam on the top of samples at a steady state under 1 sun irradiation. According to the equation (1), the radiation heat flux is calculated to be ~11 W m-2, which is ~1% of solar flux.

- Convection:

The convection heat flux is calculated via Newton' law of cooling:

Q= hAΔT                                                        (2)

where Q (W m-2) is the convection heat flux; h is the convection heat transfer coefficient, that’s about 5 W m-2 K-1 as reported[21]; A (m2) is the surface area (D46 mm); ΔT (1.6 K)is different value between the average surface temperature of samples and the ambient temperature upward the samples under 1 sun illumination. According to the equation (2), the convection heat flux is estimated to be ~8 W m-2, which is ~1% of solar flux.

- Conduction:

The conduction heat flux was calculated based on the flowing Equation:

Q=CmΔT                                                        (3)

Where Q is the heat loss; C is the specific heat capacity of water, that’s 4.2 J ℃-1 g-1; m (65 g) is the weight of water used in the paper; ΔT (1.2 ℃) is the temperature difference of pure water after and before 1 h solar irradiation under 1 sun. According to the equation (3), the conduction heat flux can be estimated to be ~54 W m-2, which is ~5% of solar flux.

Note S calculation of emissivity[19].

ε=α=1-R-T=1-1.5%-1.5%=0.97  α-absorbility, ε-emissivity.

Reference

- Q. Chen, Z. Pei, Y. Xu, Z. Li, Y. Yang, Y. Wei, Y. Ji, A durable monolithic polymer foam for efficient solar steam generation. Chem. Sci. 9 (2018) 623-628. https://doi.org/10.1039/c7sc02967e.

- H. Li, Y. He, Y. Hu, X. Wang, Commercially available activated carbon fiber felt enables efficient solar steam generation. ACS Appl. Mater. Interfaces 10 (2018) 9362-9368. https://doi.org/10.1021/acsami.7b18071.

- G. Wang, Y. Fu, X. Ma, W. Pi, D. Liu, X. Wang, Reusable reduced graphene oxide based double-layer system modified by polyethylenimine for solar steam generation. Carbon 114 (2017) 117-124. https://doi.org/10.1016/j.carbon.2016.11.071.

- S. Ma, C. Chiu, Y. Zhu, C. Tang, H. Long, W. Qarony, X. Zhao, X. Zhang, X. Lo, Y. Tsang, Recycled waste black polyurethane sponges for solar vapor generation and  distillation. Appl. Energy 206 (2017) 63-69. https://doi.org/10.1016/j.apenergy.2017.08.169.

- G. Wang, Y. Fu, A. Guo, T. Mei, J. Wang, J. Li, X. Wang, Reduced graphene oxide−polyurethane nanocomposite foam as a reusable photoreceiver for efficient solar steam generation. Chem. Mater. 29 (2017) 5629−5635. https://doi.org/10.1021/acs.chemmater.7b01280.

- C. Chen, Y. Li, J. Song, Z. Yang, Y. Kuang, E. Hitz, C. Jia, A. Gong, F. Jiang, J. Zhu, B. Yang, J. Xie, L. Hu, Highly flexible and efficient solar steam generation device. Adv. Mater. 29 (2017) 1701756. https://doi.org/10.1002/adma.201701756.

- Q. Jiang, L. Tian, K. K. Liu, S. Tadepalli, R. Raliya, P. Biswas, R. R. Naik, S. Singamaneni, Bilayered biofoam for highly efficient solar steam generation. Adv. Mater. 28 (2016) 9400. https://doi.org/10.1002/adma.201601819.

- G. Ni, N. Miljkovic, H. Ghasemi, X. Huang, S. V. Boriskina, C. Lin, J. Wang, Y. Xu, M. M. Rahman, T. Zhang, G. Chen, Volumetric solar heating of nanofluids for direct vapor generation. Nano Energy 17 (2015) 290. https://doi.org/10.1016/j.nanoen.2015.08.021.

- Y. Zeng, K. Wang, J. Yao, H. Wang, Hollow carbon beads for significant water evaporation enhancement. Chem. Eng. Sci. 116 (2014) 704. https://doi.org/10.1016/j.ces.2014.05.057.

- G. Xue, K. Liu, Q. Chen, P. Yang, J. Li, T. Ding, J. Duan, B. Qi, J. Zhou, Robust and low-cost flame-treated wood for high-performance solar steam generation. ACS Appl. Mater. Interfaces 9 (2017) 15052. https://doi.org/10.1021/acsami.7b01992.

- N. Xu, X. Hu, W, Xu , X. Li, L. Zhou, S. Zhu, J. Zhu, Mushrooms as efficient solar steam‐generation devices. Adv. Mater. 29 (2017) 1606762. https://doi.org/10.1002/adma.201606762.

- L. Zhu, M. Gao, C. Nuo Peh, X. Wang, G. Ho, Self‐Contained Monolithic Carbon Sponges for Solar‐Driven Interfacial Water Evaporation Distillation and Electricity Generation. Adv. Energy Mater. 8 (2018) 1702149. https://doi.org/10.1002/aenm.201702149.

- X. Liu, X. Wang, J. Huang, G. Cheng, Y. He, Volumetric solar steam generation enhanced by reduced graphene oxide nanofluid. Appl. Energy 220 (2018) 302–312. https://doi.org/10.1016/j.apenergy.2018.03.097.

- M. Gao, P. Nuo Connor, G. Ho, Plasmonic photothermic directed broadband sunlight harnessing for seawater catalysis and desalination. Energy Environ. Sci., 9 (2016) 3151-3160. https://doi.org/10.1039/C6EE00971A.

- H. Jin, G. Lin, L. Bai, A. Zeiny, D. Wen, Steam generation in a nanoparticle-based solar receiver. Nano Energy 28 (2016) 397-406. https://doi.org/10.1016/j.nanoen.2016.08.011.

- Y. Li, T. Gao, Z. Yang, C. Chen, W. Luo, J. Song, E. Hitz, C. Jia, Y. Zhou, B. Liu, B. Yang, L. Hu, 3D-Printed, all-in-one evaporator for high-efficiency solar steam generation under 1 sun illumination. Adv. Mater. 29 (2017) 1700981. https://doi.org/10.1002/adma.201700981.

- Q. Fang, T. Li, Z. Chen, H. Lin, P. Wang, F. Liu, A full biomass derived solar still for robust and stable evaporation to collect clean water from various water-bearing media. ACS Appl. Mater. Interfaces 11 (2019) 10672-10679. https://doi.org/10.1021/acsami.9b00291.

- G. Ni, G. Li, S. Boriskina, H. Li, W. Yang, T. Zhang, G. Chen, Steam generation under one sun enabled by a floating structure with thermal concentration. Nat. Energy 1 (2016) 16126–16132. https://doi.org/10.1038/NENERGY.2016.126.

- T. Li, Q. Fang, X. Xi, Y. Chen, F. Liu, Ultra-robust carbon fibers for multi-media purification via solar-evaporation. J. Mater. Chem. A 7 (2019) 586. https://doi.org/10.1039/c8ta08829b.

- J. Greffet, P. Bouchon, G. Brucoli, F. Marquier, Light Emission by Nonequilibrium Bodies: Local Kirchhoff Law. Phys. Rev. X 8 (2018) 021008. https://doi.org/10.1103/PhysRevX.8.021008.

- P. Zhang, Q. Liao, T. Zhang, H. Cheng, Y. Huang, C. Yang, C. Li, L. Jiang, L. Qu, High throughput of clean water excluding ions, organic media, and bacteria from defect-abundant graphene aerogel under sunlight. Nano Energy 46 (2018) 415–422. https://doi.org/10.1016/j.nanoen.2018.02.018.

- L. Zhou, Y. Tan, J. Wang, W. Xu, Y. Yuan, W. Cai, S. Zhu, J. Zhu, 3D Self-Assembly of Aluminium Nanoparticles for Plasmon-Enhanced Solar Desalination. Nat. Photonics 10 (2016) 393-398.

- R. Li, L. Zhang, L. Shi, P. Wang, MXene Ti3C2: an effective 2D light-to-heat conversion material. ACS Nano 11 (2017) 3752-3759. https://doi.org/10.1021/acsnano.6b08415.

# Text boxes

Fig. S1. Schematic fabrication process of MP and PBP-Rx.

Fig. S2. (a-c) Optical images of floating states for PP with different mass percent of PVDF; Optical images for PP with different mass percent of PVDF (inset); (d) Optical images for PP with different mass percent of PVDF.

Fig. S3. (a-c) Optical images of floating states for PP with different thickness of PU.

Fig. S4. (a) Mass change of SWP device with PP and PBP-R1.5 (with different dosage of Bi2S3) under 1 sun illumination, respectively; (b) Optical images of PBP-R1.5 (with different dosage of Bi2S3).

Fig. S6. The FE-SEM images for Rx.

Fig. S5. Schematic diagram illustrating (a) design principle of the architecture inspired by chrysanthemum and synthesis procedure of chrysanthemum-like Bi2S3 architecture; (b) The incident light can be guided into the gaps and be fully absorbed for solar thermal conversion; (c) The absorption spectra of Rx.

Fig. S7. The cross section view of temperature distributions of SWP device (a) without and (b) with PU after 1h illumination were monitored by IR camera; (c) The optical image of (ⅰ) Top and side view (ⅱ) side view of SWP device with floating PBP.

Fig. S9. (a) Transmittance and (b) reflectance spectra of R1.5, PU and PBP-R1.5, respectively.

Fig. S8. (a-c) Optical images of free floating state of ⅰ) MP; ⅱ) pristine PU; ⅲ) PBP.

Fig. S10. The optical images of (a) bending and (b) compression tests of PBP-R1.5; (c) The floating states of PBP-R1.5 before and after 24 h immersion in 2 M HCl and 2 M KOH aqueous solution.