Tables

Table 1

Properties of cemented carbide material.

| Composition | Flexural strength (MPa) | Hardness (HRA) | Density (g/cm3) | Young’s Modulus (GPa) | Thermal expansion coefficient (10-6/k) | Poisson’s ratio |
| --- | --- | --- | --- | --- | --- | --- |
| WC+Co | 1720 | 92.5 | 13.9 | 550 | 5.5 | 0.27 |

Table 2

Reaction equations of Cl2 and SF6 with WC.

| Etching gas | Reaction equation | Gibbs free energy | Whether the reaction happens |
| --- | --- | --- | --- |
| Cl2 | 2WC+7Cl2=2WCl4+C2Cl6 | -692555.8 | Yes |
|  | 2WC+8Cl2=2WCl6+C2Cl4 | -813255.802 | Yes |
|  | 2WC+9Cl2=2WCl6+C2Cl6 | -884830.564 | Yes |
|  | 2WC+9Cl2=2WCl6+2CCl3 | -654634.166 | Yes |
|  | 2WC+9Cl2=2WCl5+2CCl4 | -633810.09 | Yes |
| SF6 | WC+SF6=WF6+CS | -298471.2 | Yes |