ZIF Filled PDMS Mixed Matrix Membranes for Separation of Solvent Vapors from Nitrogen

Fatma Şahin 1, Berna Topuz2, Halil Kalıpçılar1*

1 Department of Chemical Engineering, Middle East Technical University, 06800, Ankara, Turkey

2Department of Chemical Engineering, Ankara University, 06100, Ankara, Turkey

Corresponding Author:

Halil Kalıpçılar

Tel: +90-312-210 4357

Fax: +90-312-210 2600

e-mail: kalipcil@metu.edu.tr

SUPPORTING INFORMATION

Fig. S1. N2 adsorption isotherms of ZIFs at 77 K

Fig.S2. TGA curves of (a) ZIFs (b) Pure PDMS and PES support membrane

1

4

3

2

5

Fig. S3. TGA curves of pieces of a 20 % ZIF-L/PDMS membrane.  The location of membrane pieces analyzed by TGA is schematically shown in the insert.

Figure S4. VOCs flux of PES support membrane

(d)

(c)

(b)

(a)

(e)

Figure S5. SEM image of (a) 20 % ZIF-8/PDMS, (b) 20 % ZIF-L/PDMS, (c) 20 % ZIF-

67/PDMS, (d) 20 % ZIF-7/PDMS, (e) 20 % ZIF-71 PDMS MMMs

Table S1. Solubility Parameter (δ) values of solvents

| Solvent | δD (Mpa 0.5) | δP (Mpa 0.5) | δH (Mpa 0.5) | δ (Mpa 0.5) |
| --- | --- | --- | --- | --- |
| MeOH | 14.7 | 12.3 | 22.3 | 29 |
| EtOH | 15.8 | 8.8 | 19.4 | 27 |
| 1-propanol | 16 | 6.8 | 17.4 | 25 |
| IPA | 15.8 | 6.1 | 16.4 | 24 |
| EtAc | 15.8 | 5.3 | 7.2 | 18 |

δ2= δD2 + δP2 + δH2                       Eqn S1.

δD , δP  and δH values of solvents of  taken from literature (M. Charles, Hansen Solubility Parameters: A User’s Handbook, CRC Press LLC, America, 2000).

Table S2. The measured flux of mixed matrix membrane

|  |  |  | Molar Composition VOCs : N2 = 980 : 20 |  |
| --- | --- | --- | --- | --- |
|  | Thickness (μm) | Pure N2 (GPU) | N2 (GPU) | VOCs (GPU) |
| Pure PDMS Membrane | 15.2 ± 1.1 | 17 ± 1.8 | 19 ± 2.9 | 406 ± 36.0 |
| 20 % ZIF-8 PDMS MMMs | 27.7 ± 0.9 | 10 ± 0.8 | 11 ± 0.7 | 221 ± 14.0 |
| 20 % ZIF-L PDMS MMMs | 58.5 ± 1.2 | 2 ± 0.2 | 3 ± 0.1 | 169 ± 20.2 |
| 20 % ZIF-67 PDMS MMMs | 59.2 ± 1.2 | 4 ± 0.8 | 5 ± 0.4 | 93 ± 5.1 |
| 20 % ZIF-7 PDMS MMMs | 47.0 ± 0.8 | 3 ± 0.5 | 5 ± 0.5 | 149 ± 20.5 |
| 20 % ZIF-71 PDMS MMMs | 50.3 ± 0.8 | 7 ± 1.3 | 6 ± 0.2 | 151 ± 20.6 |